## Slide 1
July 22, 2011
Steven Ehret
Anodization and In-situ Testing of Titanium Alloys for Capacitor Anodes

## Slide 2
Presentation Overview
Aims of Work
Background
Technical Design
Results and Conclusions
Future Work

## Slide 3
Acknowledgements
Dr. Frank Merat
Dr. Gerhard Welsch and Don McGervey
Dr. C.C. Liu and Laurie Dudik
US Department of Energy and ARPA-E

## Slide 4
Aims of Work
Aid Development of Materials for High Energy and Power Density Capacitors by:
    Instrumentation to create capacitor anodes while recording voltage and current data during the process
    Test platform to provide first order testing of new materials as capacitor anodes

## Slide 5
Aims of Work
Design Specifications
  Digitally programmable current source 1 – 100 mA
    Programmable compliance voltage of 0 – 30V
  Measure and record voltage across load 0 – 30V, 10 bit
  Measure and record current through load 10nA – 100mA, 10 bit
  Multiple channels
  Computer interface

## Slide 6
Background – Capacitor Overview
Capacitors
Dielectric Constant - εr
Energy
Notes: Capacitor - Energy Storage Device
Accumulation of charge  field  stored energy

## Slide 7
Background – Non-Idealities
Equivalent Series Resistance – ESR
Imperfect Insulator
  Leakage Current
  Voltage Limitations
RS
C
Notes: ESR
Heating, shortens life always
Power limitations
Imperfect Insulator
Defects allow leakage current
Will breakdown at some voltage
ESL
Mainly due to packaging, reason not discussed

## Slide 8
Background – Ti Based Anodes
High Energy and Power Density Capacitors

## Slide 9
Background – Ti Based Anodes
Performance limited by high leakage currents in previous work
  Newly developed Ti alloys are promising to reduce the leakage current to levels currently accepted by industry
Anodes created via process of anodization
Notes: 10 nA/uF*V

## Slide 10
Background - Instrumentation
Analog Control Circuitry
Analog to Digital Conversion
Microcontrollers
Software
  User Interface
  Communication
  Long Term Data Storage
10010111

## Slide 11
Technical Design
System Level Design
Preliminary Design Overviews
Final Design
  Analog Circuitry
  Digital Circuitry
  Firmware
  Software
Calibration
Test Setup

## Slide 12
System Level Design

## Slide 13
Preliminary Design Overviews
Prototype I
  Off-the-shelf data acquisition solutions
  Focus on analog front-end
  Logarithmic amplifier to achieve full dynamic range
  Barebones construction, single channel
Shortcomings
  Off-the-shelf DAQ solutions unacceptable
    Large absolute accuracy error
    High Cost

## Slide 14
Preliminary Design Overviews
Prototype II
  Microcontroller for ADC and control signals
  Focus on computer interface via UART
  Minor improvements to analog front-end
  4-layer custom PCB
Shortcomings
  Sampling rate of ADCs not fast enough
  More ADC resolution desired
  Current source limited to approximately 50 mA

## Slide 15
Final Design – Analog Circuitry
Voltage Compliance
Current Source and Control
Current Sink and Control
Current Measurement (Transimpedance Amplifier)
Voltage Measurement
Filters

## Slide 16
Voltage Compliance

## Slide 17
Current Source and Control

## Slide 18
Current Sink and Control

## Slide 19
Current Measurement

## Slide 20
Filters

## Slide 21
Final Design – Digital Circuitry
Microcontroller
Board to Computer Communication
Analog to Digital Conversion

## Slide 22
Microcontroller
ATXMEGA64A3
  Serial Communication: UART, SPI
  ADC
  General Purpose I/O

## Slide 23
Board to Computer Communication
Connects via USB
  FTDI FT232H USB to UART
2Mbaud serial connection
  Custom packet structure and protocol

## Slide 24
Analog to Digital Conversion
  2 physical, 12-bit, 1 MSa/s pipelined ADCs
  4 virtual channels per ADC
  1.22V reference voltage
  Differential Inputs

## Slide 25
Firmware

## Slide 26
Software
MATLAB used to communicate with device and record data
Limited features, intended for preliminary testing
  Fully functional GUI and data recording platform to be implemented in NI LabVIEW

## Slide 27
Calibration
Hardware
  Current Source potentiometer calibrated to 20 mA
  Current Sink potentiometer calibrated to 20 mA
Software
  ADC offset null
  Auto-zero functionality when microcontroller starts up
ADC Characterization

## Slide 28
Test Setup
Commercial aluminum electrolytic capacitors used as reference
Tested by anodizing samples of thin-film alloys of Ti, Zr, Ta, and Pb in 1% and 5% H3PO4

## Slide 29
Results and Conclusions
  Measurement Error
  Anodization Results
  Testing Results
  Conclusions

## Slide 30
Measurement Error
Sources of Error
  ADC
    INL:+/- 5 LSBs Max, +/- 2 LSBs Nominal
    Offset: +/- 2 mV
  1.22 Volt Reference
    +/- 1%
  Op-amp Input offset voltage
    2.5 mV
  Resistor Tolerances
    +/- 1%
  System Noise – Thermal, EMI, etc.

## Slide 31
Measurement Error
Mitigation of Errors
  ADC
    INL: Nothing, +/- 5 LSB error = 5/2^11 = 0.24% error
    Offset: Offset-null routine during device startup
  1.22 Volt Reference
    Auto-zero routine during device startup
  Input offset voltage
    Auto-zero routine during device startup
  Resistor Tolerances
    Auto-zero routine during device startup
  System Noise - Averaging

## Slide 32
Results
Reference

## Slide 33
Results
Anodization

## Slide 34
Results
Anodization

## Slide 35
Results
Anodization

## Slide 36
Results
Anodization

## Slide 37
Results
Anodization

## Slide 38
Results
Anodization

## Slide 39
Results
Leakage Current Measurement

## Slide 40
Results
Testing
1000uF Load 1uF Load

## Slide 41
Conclusions
Anodization function of instrumentation successful and useful to identify important characteristics of anode material for capacitors
Testing function of instrumentation only useful for large capacitive loads

## Slide 42
Future Work
Device Improvements
  Expand to 4 channel functionality from 2 channels currently
  Allow testing mode to be used for large and small capacitive loads
LabVIEW user interface
High voltage version

## Slide 43
Questions?